Stationary Diesel Engine Oils

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Pour Point C, Max. | Flash Point COC, C, Min. | Description / Application |
| --- | --- | --- | --- | --- | --- |
| Servolube 68 Servolube 100 Servolube 150 Servolube 220 | 62– 74 90– 110 135 – 165 198 - 242 | 90 90 90 90 | (-) 6 (-) 6 (-) 6 (-) 3 | 210 216 224 228 | Servolube oils are non-detergent type stationary diesel engine oils, recommended for lubrication of slow and medium speed stationary diesel engines where operating conditions do not require a detergent oil. These oils are also found to give satisfactory performance in the lubrication of reciprocating air compressors. |