SERVO ( PRODUCT DATA SHEET
                 
 

SERVO GEAR SUPER LS 90


[image: image1.jpg]IndianQil



GRADES AVAILABLE - SERVO GEAR SUPER LS 90




CHARACTERISTICS 

	SAE GRADE
	LS 90

	Kinematic Viscosity cSt @ 40(C

100(C
	200

16 – 18

	Viscosity Index, Min.
	90

	Flash point (COC), (C Min.
	180

	Pour Point, (C Max.
	(-) 9


PERFORMANCE BENEFITS


Servo Gear Super LS 90


Have exceptional chemical and thermal stability  resulting in enhanced gear and bearing life due to minimal deposits..


Provides excellent frictional characteristics for effective limited-slip performance..


Ensures outstanding rust and corrosion protection.  


Exhibits good compatability with seals and gaskets therby minimizing leakages.


Resists foaming and maintains film strength.


 





  











PERFORMANCE STANDARDS





Servo Gear Super LS 90 meet the following specifications:


API GL5  


ZF TE – ML –05








APPROVALS


Servo Gear Super LS 90 is approved by :


Bharat Earth Movers Ltd., Bangalor.




















DESCRIPTION





Servo Gear Super LS 90 is a high performance Automotive gear oil blended from specially selected high viscosity index base stocks and contain additives which impart extreme pressure, anti-rust, anti-corrosion and anti oxidation characteristics. It also contains additive system which is specially designed for “limited slip” rear drive differentials. 











 











APPLICATION





Servo Gear Super LS 90 is an effective lubricant for limited-slip differentials, final drives and axles of Off-highway earth moving equipment.  It can also be used in other automotive and industrial applications involving gears operating under low speed/high torque and high speed/ shock load conditions.  





























HEALTH & SAFETY  

These oils are unlikely to present any significant health or safety hazard when properly used in the recommended application and good standards of industrial and personal hygiene are maintained.

For further information please contact our nearest office OR :

Technical Services Dept., Indian Oil  Corporation  Ltd., G-9, Ali Yavar Jung Marg, Bandra (East), Mumbai – 400 051

                          E-Mail: tservices@indianoil.co.in    OR    tech_services@indianoil.co.in

