SERVO ( PRODUCT DATA SHEET
                 
 

SERVO XEE SJ


[image: image1.jpg]IndianQil



GRADES AVAILABLE - -SERVO XEE SJ 10W-30, 10W-40, 15W-40, 20W-50













CHARACTERISTICS 

	SAE GRADE
	10W-30
	10W-40
	15W-40
	20W-50

	Kin.Viscosity @ 100ºC, cSt
	9.5 – 11.0
	13.5 – 14.5
	13.5 - 14.5
	17.5 – 19.5

	Viscosity Index, Min
	130
	140
	130
	130

	Flash Point, COC, ºC, Min
	200
	206
	206
	206

	Pour Point, (C, Min.
	(-) 30
	(-) 27
	(-) 24
	(-) 21

	TBN, mg KOH/gm
	9 – 11
	9 – 11
	9 – 11
	9 - 11


PERFORMANCE BENEFITS


 


Superior performance in terms of improved oil and engine life.





Less oil thickening, better deposit control.





Excellent Engine Cleanliness.





Catalytic Convertor Compatible.

















PERFORMANCE STANDARDS


       


API SJ in gasoline and API CF in diesel service.





ACEA A3/B3 – 96, VW 500.00/505.00, MB 229.1





Fuel economy standards API EC II & EC I for 10W-30 and 10W-40 grade respectively.




















 





APPLICATION





Servo XEE SJ oils are recommended for new generation imported and Indian passenger cars using petrol.  





 





  








DESCRIPTION





Servo XEE SJ oils are long life, high performance fuel economy engine oil for new generation petrol and diesel vehicles.   These oils are blended from high viscosity index base stocks and contain additives to meet the highest quality performance standard











HEALTH & SAFETY  

These oils are unlikely to present any significant health or safety hazard when properly used in the recommended application and good standards of industrial and personal hygiene are maintained.

For further information please contact our nearest office OR:

Technical Services Dept., Indian Oil Corporation Ltd.,G-9,Ali Yavar Jung Marg, Bandra (E), Mumbai–400 051

                     E-Mail: tservices@indianoil.co.in    OR    tech_services@indianoil.co.in

