SERVO ( PRODUCT DATA SHEET
                 
 

SERVO GEAR HP 90 (T) / 140 (T)


[image: image1.jpg]IndianQil



GRADES AVAILABLE - SERVO GEAR HP 90 (T) / 140 (T)  



CHARACTERISTICS 

	SAE GRADE
	90 (T)
	140 (T)

	Kinematic Viscosity cSt @ 100(C
	16 – 18
	28 – 34

	Viscosity Index, Min.
	90
	90

	Flash point (COC), (C Min.
	180
	190

	Pour Point, (C Max.
	(-) 9
	0


PERFORMANCE STANDARDS





Servo Gear HP 90 (T) & 140 (T) oil meets:





API Service GL 4


IS: 1118-1992  


US MIL-L 2105











PERFORMANCE BENEFITS


 


Satisfy the lubrication requirements of a wide variety of gears.


Provide protection against wear, due to good EP characteristics


Give long service life even under high temperature operation since it has excellent oxidation stability. 


Provide good protection against corrosion.

















DESCRIPTION





Servo Gear HP 90 (T) & 140 (T) oils are an extreme pressure hypoid gear oil.  This oil is blended from selected base stocks and contain specific additive package to provide extreme pressure, anti wear characteristics.











APPLICATION





Servo Gear HP 90 (T) & 140 (T) oils are recommended for HCV, LCV transmissions of constant    synchromesh type for which are p   gear oil  

















HEALTH & SAFETY  

These oils are unlikely to present any significant health or safety hazard when properly used in the recommended application and good standards of industrial and personal hygiene are maintained.

For further information please contact our nearest office OR:

Technical Services Dept., Indian Oil Corporation Ltd.,G-9,Ali Yavar Jung Marg, Bandra (E), Mumbai–400 051

                     E-Mail: tservices@indianoil.co.in    OR    tech_services@indianoil.co.in

