SERVO ( PRODUCT DATA SHEET
                 
 

SERVOGEM ALT


[image: image1.jpg]IndianQil



GRADES AVAILABLE – SERVOGEM ALT




CHARACTERISTICS         

	NLGI GRADE
	Servogem ALT

	Colour
	Brown

	Structure
	Smooth

	Soap Type
	Lithium

	Worked Penetration @ 25(C, (60 Strokes)
	220-250

	Drop Point, (C,  Min.
	180


PERFORMANCE BENEFITS





Excellent resistance to water washout


Superior oxidation and structural stability


High degree of antirust and anticorrosion properties.


Give outstanding performance under varying operating conditions.


Suitable for lubrication under sub-zero (-25(C) to reasonably high (140(C) temperature conditions.    


Gives longer service life compares to conventional wheel bearing greases














PERFORMANCE STANDARDS





Meets specification of Association of American Railroads (AAR-M-942-81) with deviation in consistency and passes SKF Emcor corrosion test and WD-17-MISE-92 specifications.





APPROVAL:


Servogem ALT is approved by 


Ashok Leyland Ltd, Chennai-Grease change every 48000 Kms.








APPLICATION





This grease is specially developed for the lubrication of Wheel Bearings of Ashok Leyland commercial vehicles to give longer service life.   





DESCRIPTION





Servogem ALT is a premium quality, lithium soap, automotive Wheel Bearing grease.    The grease is manufactured from high viscosity index base oils and select additives with superior performance benefits.














HEALTH & SAFETY  

These oils are unlikely to present any significant health or safety hazard when properly used in the recommended application and good standards of industrial and personal hygiene are maintained.

For further information please contact our nearest office OR:

Technical Services Dept., Indian Oil Corporation Ltd.,G-9,Ali Yavar Jung Marg, Bandra (E), Mumbai–400 051

                     E-Mail: tservices@indianoil.co.in    OR    tech_services@indianoil.co.in

