### Chain Grease

| Product | Colour | Worked Penetration at 25C after 60 strokes | Drop Point C, Min | Description / Application |
| --- | --- | --- | --- | --- |
| Servo Chain Compound Servo Chain Compound (LGB) | Yellow Brown Yellow Brown | 90 – 120 (Unworked) 60 – 80 (Unworked) | 70 80 | Servo Chain Compound is recommended for lubrication of chains and is applied by dipping the chain in the molten compound so that it penetrates well in-between the narrow clearances of the pin-bush and the bush rollers. Servo Chain Compound provides resistance to formation of tight links, thereby reducing wear and elongation of chains and also protects the sprocket and transmission components against rust, corrosion and wear even in contact with high water. Servo Chain Compound (LGB) has superior antiwear properties and resistance to corrosion. |
| Rolon Servo Grease | Creamy | 355 - 385 |  | Rolon Servo Grease is specially formulated liquid chain grease for lubrication automotive chain drives. It contains volatile solvent and should be kept away from naked flame. |
| Servo Chainkote | Brown | 340 – 370 | -- | Servo Chainkote is a specially designed soap based emulsion in water for the lubrication of chains in LPG filling conveyor systems. |