Circulating and Hydraulic Oils (R&O Type)

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servocirol 32 Servocirol 46 Servocirol 68 Servocirol 100 Servocirol 150 | 29 - 35 42 - 50 62 - 74 90 - 110 135 - 165 | 95 95 95 90 90 | 196 200 210 210 230 | Servocirol oils are premium quality R&O type hydraulic oils formulated with superior quality hydro treated base stocks Servocirol meet IS:3098-1983 (Reaffirmed 2004), DIN-51524 H and HL (except for very low pour point) and US Steel 135 requirements. Servocirol 32, 46, 68 and 150 also meet Cincinnati Machines, U.S.A. specification P-38, P-55, P-54 and P-57 respectively. Servocirol oils are recommended for hydraulic system, circulation system of industrial gearboxes, air compressors requiring turbine quality oil and for plain and anti-friction bearings of turbo feed pumps, turbo blowers, etc. These Oils can be used for lubrication of intermittently operating turbo generator sets where oil is changed after short duration. |