Cup Greases

| Product | Colour | Worked Penetration at 25C after 60 strokes | Drop Point C, Min | Description / Application |
| --- | --- | --- | --- | --- |
| Lubrex Cup Grease 2 Lubrex Cup Grease 3 | Brown Yellow Brown | 260 – 300 220 – 250 | 100 95 | Lubrex Cup Greases are smooth structured calcium soap greases possessing good water repellent characteristics. These greases are recommended widely for plain bearings operating under moderate to low temperatures and where the churning and vibrations are not excessive. |