Energy Efficient Industrial Gear Oils

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servomesh EE 150 Servomesh EE 220 Servomesh EE 257 Servomesh EE 320 Servomesh EE 460 Servomesh EE 680 | 135 – 165 198 - 242 250 – 280 288 – 352 414 - 506 612 - 748 | 90 90 90 90 90 90 | 204 232 232 232 232 232 | Servomesh EE oils are energy efficient gear oils, which provide reduced friction and thereby reduce power consumption Recommended for all types of enclosed gear drives, heavily loaded bearings and industrial gears running at high speeds, high pressures, and under impact load. Servomesh EE Gear Oils meet US Steel 224, AGMA 250-04, IS 8406, IPSS 1-09-003, David Brown S1.53.101. |