Foodgrade Greases

| Product | Colour | Worked Penetration at 25C after 60 strokes | Drop Point C, Min | Description / Application |
| --- | --- | --- | --- | --- |
| Servogrease FG 2 Servogrease FG EP 2 | Off-white Colourless | 265 – 295 265 – 295 | 250 250 | Servogrease FG are general purpose synthetic grease for food processing industry. These products have been developed by incorporating a specialised FDA approved raw materials and additives. They are listed by National Sanitary Foundation (NSF), USA as food grade lubricants type H 1 for applications where the grease may have incidental food contact. |