### Graphited Greases

| Product | Colour | Worked Penetration at 25C after 60 strokes | Drop Point C, Min | Description / Application |
| --- | --- | --- | --- | --- |
| Servogrease Graphited 4080 | Black | 300 – 350 | 88 | Aluminium Stearate grease compounded with Graphite. It meets the IS: 408 specification and is used for corrosion prevention of ERC (Elastic Rail Clips) of Railway tracks. |
| Servogrease Graphited 5081 Servogrease Graphited 5082 Servogrease Graphited 5083 | Black Black Black | 310 – 340 265 – 295 175 – 205 | 95 100 95 | Servogrease Graphited is recommended for general lubrication under comparatively high load and low relative displacement of inter-acting surfaces. These greases meet IS: 508-1987 (Reaffirmed 1993) specifications for Grade 1, Grade 2 & Grade 3 respectively. These greases are recommended for leaf springs, hydraulic rams, plungers, slides, elevator cables, pantograph pans, steel wire ropes & certain anti-seize purposes. |