### Machine Tool Way Oils

| Product | Kin. Viscosity cSt at 40ºC | VI Min. | Flash Point COC, ºC, Min. | #### Description / Application |
| --- | --- | --- | --- | --- |
| Servoway 32 Servoway 68 Servoway 100 Servoway 220 | 29 – 35 62 – 74 90 – 110 198 - 242 | - - - - | 160 170 170 190 | Servoway oils have tackiness, anti-rust and anti-foam additives enabling higher loading of machine tools, minimum stick-slip and chatter, and provide improved surface finish to the job. These oils protect parts against rust and corrosion and reduce oil consumption due to good adhesive characteristics. Servoway 68 and 220 meet ASLE standard W 315 and W 1000 as well as Cincinnati Machines specifications P-47 and P-50 respectively. These oils are excellent products for slide way lubrication of planers, grinders, horizontal boring machines, shapers, jig borers etc., involving high precision work and are also recommended for lubrication of gears by oil-can. |