Synthetic Greases

| Product | Colour | Worked Penetration at 25C after 60 strokes | Drop Point C, Min | Description / Application |
| --- | --- | --- | --- | --- |
| Servogrease SHC 600 | Black | 265 – 295 | 260 | Servogrease SHC 600 is a semi synthetic base oil grease containing balanced additives and solid lubricant suitable for centralized lubrication system for very high temperature application in Steel, Aluminium, Cement, Mining industries. |
| Servoplex SHC 120 Servoplex SHC 460 | Light Brown Light Brown | 265 - 295 290 – 320 | 250 260 | Servoplex SHC greases are lithium complex soap grease formulated with synthetic hydrocarbon base fluids and fortified with selected additives for superior performance under high load and varying temperature conditions. They have excellent thermal and oxidation stability, resistance to water and provide excellent protection against wear and corrosion and longer service life. |