# GRADES AVAILABLE – SERVO EICHER DIFFERENTIAL OIL

# CHARACTERISTICS

| SAE GRADE | Eicher Differential Oil |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 28 – 34 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), (C Min. | 180 |
| Pour Point, (C Max. | 0 |

# Text boxes

# PERFORMANCE BENEFITS

Servo Eicher Differential oil

- Has exceptional chemical and thermal stability permitting use upto bulk oil temperature of 150(C

- Has excellent extreme pressure property to give maximum protection against low speed-high torque wear and high speed – shock induced scoring

- Guard automotive gear assemblies against rust and corrosion

# PERFORMANCE STANDARDS

Servo Eicher Differential oil meet the following specifications:

- API Service GL5

- IS 118-1992, EP Type GL-5, SAE 140 viscosity grade

- US Military MIL-L-2105D

- UK Defence CS 3000B

# MANUFACTURERS APPROVAL

Servo Eicher Differential oil is approved M/s Eicher Motors as Genuine Oil.

DESCRIPTION

Servo Eicher Differential Oil is an automotive extreme pressure automotive oil blended from specially selected high viscosity index base stocks and contain additives which impart extreme pressure, anti-rust, anti-corrosion and anti oxidation characteristics.  This oil is specifically formulated to meet the  rigorous service demand of commercial fleet mechanical transmissions, axles and gear boxes.

# APPLICATION

Servo Eicher Differential Oil is primarily recommended for the lubrication of hypoid differential units operating under severe conditions and other types of mechanical transmissions and drive axles where extreme pressure gear oils are required.