# GRADES AVAILABLE – HYUNDAI SERVO BRAKE OIL

# CHARACTERISTICS

| Appearance | Clear Homogeneous red liquid |
| --- | --- |
| Equilibrium Reflex Boiling Point, (C Min. | 205 |
| Kinematic Viscosity, cSt @ (-) 40 (C, Max. @ 100 ( C, Min. | 1500 1.5 |
| pH Value | 7.0-11.5 |

# Text boxes

# PERFORMANCE BENEFITS

Hyundai Servo Brake Oil

- Provides very high safety factor during driving at high speed in city and under heavy load in hilly regions

- Provides excellent protection against corrosion to iron, non-ferrous metals and zinc alloys

- Has longer service life, due to excellent oxidation stability

MANUFACTURERS APPROVAL

Hyundai Servo Brake Oil is approved by Hyundai Motors India Ltd., for exclusive use in Hyundai vehicles like Santro cars, etc.

DESCRIPTION

Hyundai Servo Brake Oil is heavy duty hydraulic brake fluid which ensures long service life of the brake fluid and components of brake mechanism. It remains clear and uniform fluid under extreme cold climatic conditions, enabling satisfactory operation of brake systems.   It also lubricates the moving parts of the brake system very effectively.

# APPLICATION

Hyundai Servo Brake Oil is recommended for hydraulic brake systems of Hyundai vehicles.

The higher boiling point of this product provided greater safety factor while driving at high speed with heavy load or in hilly areas where frequent braking generates higher temperatures in the brake system.