# GRADES AVAILABLE - SERVO 2W GEAR OIL

# CHARACTERISTICS

| SAE GRADE | 40 |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 13 –15 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), (C Min. | 226 |
| Pour Point, (C Max. | (-) 6 |

# Text boxes

#### APPROVAL

Approved for the following Moped Gear Boxes by M/s. TVS Motor Company Ltd.

- TVS XL Super

- TVS XL Super (Heavy Duty)

# PERFORMANCE BENEFITS

- Satisfy the lubrication requirements of   gears in 2 stroke  2 wheelers

- Provide protection against wear.

- Give long service life even under high temperature operation since it has excellent oxidation stability.

- Provide good protection against corrosion.

DESCRIPTION

Servo 2W Gear Oil oils are used as gear lubricants.  These oils are blended from selected base stocks and contain specific additive package to provide anti-wear, anti-rust and anti-corrosion characteristics.

# APPLICATION

Servo 2W Gear oils are recommended for Gear Lubrication of  2 wheelers.