GRADES AVAILABLE – SERVO PRIDE SUPER 15W-40, 20W-50

# CHARACTERISTICS

| SAE GRADE | 15W-40 | 20W-50 |
| --- | --- | --- |
| Kinematic Viscosity @ 100(C, cSt | 13.5 – 15.5 | 16.3 – 17.3 |
| Viscosity Index, Min | 135 | 125 |
| Flash Point, COC, (C, Min | 200 | 200 |
| TBN, mg, KOH/gm | 14 - 16 | 14 - 16 |

# Text boxes

# PERFORMANCE BENEFITS

- Increased oil drain period with potential of 45,000 kms under ideal operating conditions.

- Enhanced engine life

- Ensures increased engine cleanliness

- Reduced wear

- All weather oil

- Low oil top up

# PERFORMANCE STANDARDS

- ACEA - E5 - 02

- E-DL 4 OF IS:13656-1993

- MB 228.3

# APPLICATION

Servo Pride Super 15W-40 is recommended for all types of diesel powered vehicles ranging from light commercial vehicles to heavy duty turbo charged diesel engines and also suitable for off-highway equipment and power generation sets operating on high speed diesel.

DESCRIPTION

Servo Pride Super 15W-40 is a premium quality “Super High Performance Diesel Engine Oil” (SHPDO).    It is blended with high quality base stocks and carefully selected additives to meet the stringent requirements of various OEMs.