# GRADES AVAILABLE - SERVO PRIDE TC 15W-40

#### CHARACTERISTICS

| SAE GRADE | 15W-40 |
| --- | --- |
| Kinematic Viscosity, cSt @ 100(C | 14.0 – 15.0 |
| Viscosity Index, Min. | 135 |
| TBN, mg KOH/g | 8.5 – 11.5 |
| Flash Point, (COC)(C, Min. | 200 |
| Pour Point (C, Max. | (-) 24 |

# Text boxes

# PERFORMANCE BENEFITS

- Reduced engine scuffing & bore polishing.

- High engine cleanliness.

- Maximum protections from wear and deposits.

- Suitable for mixed fleet operation.

- Improved control of oil consumption.

- Easier cold starting.

- Excellent all weather performance due to improved cold weather properties.

- Catalytic Converter compatible.

# PERFORMANCE STANDARDS

*	API CF-4 / SG

*	MB 228.1

DESCRIPTION

Servo Pride TC 15W-40 is a premium quality, commercial multipurpose diesel engine oil. The oil is designed for the most severe performance requirements of modern, highly rated turbo charged diesel engines for the  road transport fleet applications.  It assures outstanding protection against high temperature engine deposits, oil degradation, oil thickening and corrosion resistance. The oil is having excellent shear stability to maintain viscosity under severe, high temperature operations.

# APPLICATION

Servo Pride TC 15W-40 is recommended for   commercial diesel vehicles for both National and International Heavy duty highway equipments. This oil meets API CG-4 / SG service classification for modern and low emission diesel engines.   This oil is also recommended for Gasolene Engines allowing to be used in mixed fleet operations.