# GRADES AVAILABLE - -SERVO SUPERIOR XEE 10W-30, 10W-40, 15W-40, 20W-50

# CHARACTERISTICS

| SAE GRADE | 10W-30 | 10W-40 | 15W-40 | 20W-50 |
| --- | --- | --- | --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 9.5 – 11.5 | 13.5 – 15.5 | 13.5 – 15.5 | 17.5 – 19.5 |
| Viscosity Index, Min. | 135 | 140 | 135 | 115 |
| Flash Point, COC, ºC, Min | 200 | 190 | 200 | 200 |
| Pour Point, ºC, Max | (-) 27 | (-) 27 | (-) 24 | (-) 21 |
| TBN, mg KOH/gm | 6.0 – 8.0 | 8 – 10.5 | 10.2 – 12.0 | 7.0 – 8.5 |

# Text boxes

# PERFORMANCE BENEFITS

- Superior performance in terms of oxidation stability, dispersancy characteristics and energy efficiency.

- Excellent sludge control and extra wear protection at high temperatures and severe operating conditions.

- Outstanding overall engine cleanliness and also provide long engine life.

- Fuel savings and low oil top up.

- Catalytic Converter Compatible.

# PERFORMANCE STANDARDS

- API SG

DESCRIPTION

Servo Superior XEE oils are high performance engine oil for new generation petrol and diesel vehicles.   These oils are blended from high viscosity index base stocks and contain additives to meet the stated performance standards.

# APPLICATION

Servo Superior XEE oils are recommended for new generation passenger cars using petrol and diesel.