# GRADES AVAILABLE – SERVO ULTRA 40 RR

# CHARACTERISTICS

| SAE GRADE | 40 |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 14 – 16 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), (C Min. | 226 |
| Pour Point, (C Max. | (-) 15 |
| TBN mg KOH/gm | 9.5 – 11.5 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Ultra RR oil meet specification

1051/91 of MTU, Germany

# PERFORMANCE BENEFITS

Servo Ultra RR oil is

- Effectively combat the deleterious products of combustion associated with high sulphur diesel, thus minimising deposits and wear.

- Maintain excellent engine cleanliness.

- Minimise deposits resulting from high output, low speed, low temperature operations.

- Provide excellent control of cold sludge and corrosive wear.

- Possess excellent oxidation stability ensuring long service life especially in transmission systems.

DESCRIPTION

Servo Ultra 40 RR have high detergency and excellent oxidation stability diesel engine oil recommended for engines in Marine applications and in stationary power generating sets.

# APPLICATION

Servo Ultra RR is recommended as engine oil for MTU engines in Marine applications and in stationary power generating sets.