# GRADES AVAILABLE - SERVO SYNCHRO 80W-90

# CHARACTERISTICS

| SAE GRADE | 80W-90 |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 14 –16 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), (C Min. | 180 |
| Pour Point, (C Max. | (-) 27 |
| Copper Corrosion @ 121(C, 1 hr, Max | 1 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Synchro meets:

- API Service GL 4

# PERFORMANCE BENEFITS

Servo Synchro

- Provide protection against wear, due to good EP characteristics

- Give long service life even under high temperature operation since it has excellent oxidation stability

- Provide good protection against corrosion.

- Extended oil drain interval.

DESCRIPTION

Servo Synchro is extreme pressure automotive gear oil.  This oil is blended from selected base stocks and contain special additives to provide extreme pressure characteristics for wear protection.

# APPLICATION

Servo Synchro  oil is recommended for synchromesh gear box and transfer case of light, medium and heavy commercial vehicles like bus, trucks, etc.