# GRADES AVAILABLE - SERVO FORCE BRAKE FLUID DOT 4

# CHARACTERISTICS

| Appearance | Clear Homogeneous red liquid |
| --- | --- |
| Equilibrium Reflex Boiling Point, (C Min. | 240 |
| Kinematic Viscosity, cSt @ (-) 40 (C, Max. @ 100 ( C, Min. | 1300 2.0 |
| pH Value | 8.5 - 10.5 |

# Text boxes

# PERFORMANCE BENEFITS

Servo Force Brake Fluid DOT 4

- Provides very high safety factor during driving at high speed in city and under heavy load in hilly regions

- Provides excellent protection against corrosion to iron, non-ferrous metals and zinc alloys

- Has longer service life, due to excellent oxidation stability

# PERFORMANCE STANDARDS

Servo Force Brake Fluid DOT 4

- Exceeds FMVSS  No.  116 -  DOT 3

- Meets JIS – J – 2233 / 89

DESCRIPTION

Servo Force Brake Fluid DOT 4  is heavy duty hydraulic brake fluid which ensures long service life of the brake fluid and components of brake mechanism. It remains clear and uniform fluid under extreme cold climatic conditions, enabling satisfactory operation of brake systems. It also lubricates the moving parts of the brake system very effectively.

# APPLICATION

Servo Force Brake Fluid DOT 4 is designed for use in modem brake system of automotive vehicles operating in heavy duty conditions  The higher boiling point of this product provided greater safety factor while driving at high speed with heavy load or in hilly areas where frequent  braking generates higher temperatures in the brake system.

Servo Force Brake Fluid DOT 4 is recommended for various hydraulic brake systems including disc type.