# GRADES AVAILABLE - SERVO GEAR ALT 90

# CHARACTERISTICS

| SAE GRADE | ALT 90 |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 16 – 18 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), (C Min. | 180 |
| Pour Point, (C Max. | (-) 9 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Gear ALT 90  oil meets:

- API Service GL 4

#### APPROVAL

- Ashok Leyland Ltd., Chennai – Oil change period every 40,000 KMs

# PERFORMANCE BENEFITS

- Satisfy the lubrication requirements of a wide variety of gears.

- Provide protection against wear, due to good EP characteristics

- Give long service life even under high temperature operation since it has excellent oxidation stability.

- Provide good protection against corrosion.

DESCRIPTION

Servo Gear ALT 90 oil is an extreme pressure automotive gear lubricant.  This oil is blended from selected base stocks and contain specific additive package to provide extreme pressure, anti-rust-corrosion characteristics.  This formulation has been specially developed for Syncromesh  Transmission of Ashok Leyland vehicles.

# APPLICATION

Servo Gear ALT 90 oil is recommended for Syncromesh transmission of Ashok Leyland passenger and good carriers