# GRADES AVAILABLE - SERVO HMT PREMIUM TRACTOR OIL

#### CHARACTERISTICS

| SAE GRADE | 15W-40 |
| --- | --- |
| Kinematic Viscosity, cSt @ 100(C | 14.0 – 15.0 |
| Viscosity Index, Min. | 135 |
| TBN, mg KOH/g | 9.5 – 11.5 |
| Flash Point, (COC)(C, Min. | 200 |
| Pour Point (C, Max. | (-) 24 |

# Text boxes

# PERFORMANCE BENEFITS

# Reduced engine scuffing & bore polishing.

# High engine cleanliness.

# Maximum protection from wear &  deposits

# Suitable for mixed fleet operation.

# Improved control of oil consumption.

# Easier cold starting.

# Excellent all weather performance due to improved cold weather properties.

# Catalytic Converter compatible.

# PERFORMANCE STANDARDS

*	API CF4 / SG

*	MB 228.1

*	ED-L-5 of IS : 13656 - 2002

###### MANUFACTURERS APPROVAL

Approved as Genuine Oil for HMT Tractors

DESCRIPTION

Servo HMT Premium Tractor Oil is a premium quality, genuine engine oil for HMT Tractors.   The oil is designed for the most severe performance requirements of modern, highly rated turbo charged diesel engines. It assures outstanding protection against high temperature engine deposits, oil degradation, oil thickening and corrosion resistance. The oil is having excellent shear stability to maintain viscosity under severe, high temperature operations.

# APPLICATION

Servo HMT Premium Tractor Oil is recommended for engines of HMT Tractors.