# GRADES AVAILABLE – SERVO HYDRAULIC ALT 32

# CHARACTERISTICS

| GRADE | 32 |
| --- | --- |
| Kinematic Viscosity, cSt @ 40(C | 29-33 |
| Viscosity Index, Min | 95 |
| Flash Point (COC), (C Min. | 190 |
| Pour Point, (C Max. | (-) 6 |
| Rust Test, (D-665 A&B, 24 hrs.) | Pass |

# Text boxes

# PERFORMANCE STANDARDS

- IS: 10522:1983 ( Reaffirmed 1993 )

MANUFACTURERS APPROVAL

- Ashok Leyland Ltd., Chennai.

# PERFORMANCE BENEFITS

## Servo Hydraulic ALT 32

- Provides good wear- protection, thereby prolonging service life of moving parts

- Possess high film strength properties which help minimise friction and wear

- Provide rust-protection, to reduce the incidence of corrosion

- Have excellent resistance to oxidation thereby giving long service life

- Have reduced tendency to foam thereby minimise the chance of noisy operation and erratic actuator response

DESCRIPTION

Servo Hydraulic ALT 32 is an anti-wear hydraulic and circulation oil specially formulated for efficient lubrication of a wide variety of hydraulic power packs industrial equipment. Servo Hydraulic ALT 32 is blended from highly refined base stocks and carefully selected antioxidant, anti-wear, anti-rust and anti-foam additives.

# APPLICATION

Servo Hydraulic ALT 32 is recommended as fluid media for hydraulic systems of Ashok Leyland tippers.