# GRADES AVAILABLE - SERVO POWER STEER ALT

# CHARACTERISTICS

| Colour | Red |
| --- | --- |
| Kinematic Viscosity, cSt @ 100(C | 7.4.-7.9 |
| Viscosity Index, Min | 160 |
| Flash Point (COC), (C, Min. | 180 |
| Pour Point, (C, Max. | (-) 39 |

# Text boxes

# PERFORMANCE BENEFITS

Servo Power Steer ALT

- Prvides smooth, chatter-free clutch engagement and keeps automatic transmissions operating smoothly

- Ensures long trouble free life of gears, bearings and other lubricated parts

- Minimises formation of sludge and varnish, thus maintains the system clean

- Protects parts against rusting even during idle period.

# PERFORMANCE STANDARDS

Servo Power Steer ALT meets the following specification:

- General Motor’s Type A suffix A

- Daimler Benz DBL 6623-10

- TES-122 of DDA, a Division of GM, USA

- TEML 03 of ZF, West Germany

# MANUFACTURERS APPROVAL

- Ashok Leyland Ltd., Chennai – Oil change period every 80000 KMs.

DESCRIPTION

Servo Power Steer ALT is formulated to meet power Steering fluid requirement of Ashok Leyland vehicles .  This fluid imparts anti-oxidation, anti-wear, dispersancy, defoaming and desired friction characteristics.  Due to its high viscosity index and low pour point it assures quiet and smooth operation of hydraulic equipment under all climatic conditions.  It is a fluid with low co-efficient of friction thus permitting clutch plates to engage slowly and gradually as the transmission shifts.  The fluid is compatible with seal materials, generally used in transmission systems.

# APPLICATION

Servo Power Steer ALT is recommended as Power Steering fluid for Ashok Leyland vehicles.